Supplementary Materials

Impact-resistant shear stiffening composite foam for safe battery pack

Yuxin Xia a, f, Bing Liu a, g*, Jianpeng Wu a, Zimu Li a, Quan Liu a, Jianyu Zhou a, Xixiang Lv d, Sheng Cheng d, Xin Liang e, Xiang Li f, Huaxia Deng a, c*, Xinglong Gong a, b*

a CAS Key Laboratory of Mechanical Behavior and Design of Materials, Department of Modern Mechanics, University of Science and Technology of China (USTC), Hefei, Anhui 230027, PR China

b State Key Laboratory of Fire Science, University of Science and Technology of China (USTC), 96 Jinzhai Road, Hefei, Anhui 230026, PR China

c State Key Laboratory of Nonlinear Mechanics, Institute of Mechanics, Chinese Academy of Science, 15 Beisihuan West Road, Beijing 100190, PR China

d Department of Simulation Engineering, Hefei Gotion High-Tech Power Energy Co., Ltd., Hefei, Anhui, 230011, PR China

e School of Energy Materials and Chemical Engineering, Hefei University, Hefei, 230000, PR China

f Advanced Institute for Ocean Research, Southern University of Science and Technology, Shenzhen, 518055, PR China

g Anhui Weiwei Rubber Part Group Co. Ltd., Tongcheng, Anhui, 231460, PR China

*Corresponding Author

Email address: E-mail: bingliu@ustc.edu.cn (B. Liu), hxdeng@ustc.edu.cn (H. X. Deng), gongxl@ustc.edu.cn (X. L. Gong).

The supplementary materials include:

Fig. S1 to Fig. S29

Table S1 to Table S5

Movie S1. SAE protection of glass sheets in the 50 cm height drop test.

Movie S2. SAE not penetrated at 180 km/h projectile entry velocity.

Movie S3. SAE combustion test under alcohol lamp flame.

Movie S4. Combustion test of SSG/EVA under alcohol lamp flame.

Movie S5. Flame retardant level tested by SAE through vertical combustion method.

Fig. S1. The following diagram illustrates the preparation process of SAE foams.

Fig. S2. Physical photograph of SAE foams.

Fig. S3. SAE under an optical microscope.

Fig. S4. Rheological data measured for five sets of SSG samples.

Fig. S5. Curve of storage modulus versus frequency for SSG at temperatures ranging from 15°C to 65°C.

Fig. S6. X-ray photoelectron spectroscopy of SAE foams.

Fig. S7. Density and strength of samples prepared with different SSG-to-EVA ratios.

Fig. S8. The compressive properties of five sets of SAE samples were tested at strain rates of 0.003 s-1, 0.033 s-1, 0.066 s-1, and 0.1 s-1, respectively.

Fig. S9. Area of stress-strain hysteresis curves for SAE foams.

Fig. S10. Stress-strain curve for 500 cycles at a strain rate of 0.01 s⁻¹ with 50% compression, including energy dissipation and peak stress values at the 1st, 50th, 100th, 300th, and 500th cycles.

Fig. S11. Stress-strain curves of SAE specimens measured using the Hopkins bar at different strain rates.

Fig. S12. Force-displacement curves from five sets of repeated experiments where a 5mm-thick SAE sample was dropped from heights of 10cm, 30cm, 50cm, and 70cm.

Fig. S13. Impulse decay rates of EVA and SAE at drop heights of 10 cm, 30 cm, 50 cm, and 70 cm.

Fig. S14. Residual force curves measured in experiments on SAE foams with pearl wool, EVA foam, rigid EVA foam and glass protection in the bare state.

Fig. S15. Residual velocity of a bullet after penetrating silicone foam.

Fig. S16. Residual force values of SSG/EVA foams in five drop tests.

Fig. S17. Residual force values of SAE foams in five drop hammer tests.

Fig. S18. Stress-strain curves of SSG/EVA and SAE foams.

Fig. S19. Surface morphology of SSG/EVA and SAE after burning.

Fig. S20. Residual force values of the drop hammer test after 0 s, 40 s, 60 s, 80 s, and 100 s of combustion on an alcohol lamp flame.

Fig. S21. SEM images of residual coke of SAE foams after treatment at 900 ℃.

Fig. S22. Derivative of Thermal Gravity (DTG) curves for SSG, SSG/APP, SSG/EVA and SAE.

Fig. S23. Electron microscope image of residual carbon residue from SAE at 800°C, along with distribution maps of phosphorus and silicon elements.

Fig. S24. Commercial EVA foam shrinks and curls at 300 ℃.

Fig. S25. Surface morphology of SAE foam under high temperature of 300 ℃.

Fig. S26. The energy storage modulus curve of the SAE sample obtained from compression testing at 120–150°C with a frequency of 0.1 Hz.

Fig. S27. Residual force value curves for conventional pack and pack with SAE in two consecutive hammer tests.

Fig. S28. Force-displacement curves of pack with SAE in two drop tests.

Fig. S29. Photograph of battery pack after failure during drop hammer test.

Table S1. Formulation compositions of SSG, SSG/APP, SSG/EVA, and SAE.

| Sample | Component | Weight percent (wt%) | parts per hundred (phr) |
| --- | --- | --- | --- |
| SSG | Boric acid | 96.77% | - |
|  | Silicone oil | 3.23% | - |
|  | N-octanoic acid | 250 μL / 100 g silicone oil | - |
| SSG/APP | SSG | 45% | 100 phr (based on SSG) |
|  | Ammonium polyphosphate (APP) | 55% | 122.2 phr (relative to SSG) |
| SSG/EVA | SSG | 38.54% | 100 phr (based on EVA) |
|  | Ethylene-vinyl acetate (EVA) | 38.54% | 100 phr |
|  | Azodicarbonamide (AC) | 3.85% | 10 phr (based on EVA) |
|  | Vinyl-modified silicone rubber (VMQ) | 16.53% | 42.9 phr (based on SSG) |
|  | Benzoyl peroxide (BPO) | 2.20% | 5.7 phr (based on SSG) |
|  | Diisopropyl peroxide (DCP) | 0.54% | 1.4 phr (based on EVA) |
|  | Zinc oxide (ZnO) | 0.58% | 1.5 phr (based on EVA) |
| SAE | SSG | 26.21% | 100 phr (based on EVA) |
|  | Ethylene-vinyl acetate (EVA) | 26.21% | 100 phr |
|  | Azodicarbonamide (AC) | 2.62% | 10 phr (based on EVA) |
|  | Vinyl-modified silicone rubber (VMQ) | 11.25% | 42.9 phr (based on SSG) |
|  | Benzoyl peroxide (BPO) | 1.49% | 5.7 phr (based on SSG) |
|  | Diisopropyl peroxide (DCP) | 0.37% | 1.4 phr (based on EVA) |
|  | Zinc oxide (ZnO) | 0.39% | 1.5 phr (based on EVA) |
|  | Ammonium polyphosphate (APP) | 31.98% | 122.2 phr (relative to SSG) |

Table S2. Drop weight test system parameters (Fig. 2b-2e).

| Parameter | Specification |
| --- | --- |
| Impactor mass | 0.54 kg |
| Impactor nose geometry | Cylindrical flat-end, diameter 25 mm |
| Drop heights | 10 cm, 30 cm, 50 cm, 70 cm (as annotated in respective figures) |
| Support conditions | Samples placed freely on force transducer surface |
| Boundary conditions | Unconstrained lateral movement allowed |
| Number of replicates | n = 5 for all test conditions |

Table S3. Vertical burning test results summary.

| Specimen | After-Flame Time (t1/t2) (s) | After-Glow Time (s) | Dripping | Cotton Lgnition |
| --- | --- | --- | --- | --- |
| 1 | 3/2 | 0 | No | No |
| 2 | 7/3 | 0 | No | No |
| 3 | 7/0 | 1 | No | No |
| 4 | 6/3 | 2 | No | No |
| 5 | 1/1 | 0 | No | No |

Note: t1 and t2 refer to the after-flame times after the first and second flame applications, respectively.

Table S4. Elemental analysis of carbon residue remaining in SAE at 800 °C.

| Element | wt% | Atomic percentage |
| --- | --- | --- |
| C | 4.86 | 8.20 |
| O | 48.49 | 61.38 |
| Si | 14.04 | 10.12 |
| P | 29.65 | 19.38 |
| Cu | 0.06 | 0.02 |
| Zn | 2.90 | 0.90 |
| Total: | 100.00 | 100.00 |

Table S5. SAE vertical thermal conductivity test results.

| Specimen | Thermal conductivity (W/(m·K)) | Average (W/(m·K)) |
| --- | --- | --- |
| 1 | 0.182 | 0.179 |
| 2 | 0.179 |  |
| 3 | 0.177 |  |

References

- Chen YQ, Kang YQ, Zhao Y, et al. A review of lithium-ion battery safety concerns: The issues, strategies, and testing standards. J. Energy Chem. 2021;59:83-99.

- He MN, Hector Jr LG., Dai F, et al. Industry needs for practical lithium-metal battery designs in electric vehicles. Nat. Energy 2024;9:1199-1205.

- Jin HC, Xin S, Chuang CH, et al. Black phosphorus composites with engineered interfaces for high-rate high-capacity lithium storage. Science 2020;370:192-197.

- Masalkovaitė K, Gasper P, Finegan DP. Finegan. Predicting the heat release variability of Li-ion cells under thermal runaway with few or no calorimetry data. Nat. Commun. 2024;15:8399.

- Feng XN, Ouyang M, Liu X, et al. Thermal runaway mechanism of lithium ion battery for electric vehicles: A review. Energy Storage Mater. 2018;10:246-267.

- Santosa SP., Nirmala, T. Numerical and experimental validation of fiber metal laminate structure for lithium-ion battery protection subjected to high-velocity impact loading. Compos. Struct. 2024;332:117924.

- Feng XN, Fang M, He XM, et al. Thermal runaway features of large format prismatic lithium ion battery using extended volume accelerating rate calorimetry. J. Power Sources 2014;255:294-301.

- Wang J, Feng XN, Yu YZ, et al. Rapid temperature-responsive thermal regulator for safety management of battery modules. Nat. Energy 2024;9:939–946.

- Wang WW, Dai SJ, Zhao WJ, et al. Design optimization of a novel negative Poisson's ratio non-module battery pack system considering crashworthiness and heat dissipation. Compos. Struct. 2021;275:114458.

- Longchamps RS, Ge S, Trdinich ZJ, et al. Battery electronification: intracell actuation and thermal management. Nat. Commun. 2024;15:5373.

- Xia Y, Wierzbicki T, Sahraei E, et al. Damage of cells and battery packs due to ground impact. J. Power Sources 2014;​267:78-97.

- Kukreja J, Nguyen T, Siegmund T, et al. Crash analysis of a conceptual electric vehicle with a damage tolerant battery pack. Extreme Mech. Lett. 2016;9:371-378.

- He JQ, Lu CH, Jiang HB, et al. Scalable production of high-performing woven lithium-ion fibre batteries. Nature 2021;597:57-63.

- Galos J, Pattarakunnan K, Best AS, et al. Energy storage structural composites with integrated lithium-ion batteries: A review. Adv. Mater. Technol. ​2021;6:2001059.

- Wu CX, Sun YL, Tang H, et al. A review on the liquid cooling thermal management system of lithium-ion batteries. Appl. Energy 2024;375:124173.

- Nema PK, Vijaya, Muthukumar P, et al. Recent advancements and future prospects in lithium-ion battery thermal management techniques. Energy Storage 2024;6:e70076.

- Pal SK, Singh S, Singh H, et al. Intelligent design optimization of battery pack enclosure for electric vehicle by considering cold-spraying as an additive manufacturing technology. Energy Storage 2020;2:e148.

- Ma XY, Zhang WK, Yin Y, et al. Multi-objective optimization of lithium-ion battery designs considering the dilemma between energy density and rate capability. Energy and AI 2024;18:100416.

- Zhang JF, Wang HQ, Sun WX, et al. Surface modification on ammonium polyphosphate and its enhanced flame retardancy in thermoplastic polyurethane. Polym Adv Technol. 2021;32:2879–2886.

- Jia ZZ, Jin KQ, Mei WX, et al. Advances and perspectives in fire safety of lithium-ion battery energy storage systems. eTransportation 2025;24:100390.

- Saraogi AK, Ibrahim M, Sangeethkumar E, et al. Battery materials for electric vehicle – A comprehensive review. Mater. Today: Proc 2023;72:2206-2211.

- Rana S, Kumar R, Bharj RS. Current trends, challenges, and prospects in material advances for improving the overall safety of lithium-ion battery pack. Chem. Eng. J. 2023;463:42336.

- Song YH, Wu KJ, Zhang TW, et al. A Nacre-Inspired Separator Coating for Impact-Tolerant Lithium Batteries. Adv. Mater. 2019;31:1905711.

- Attia PM, Moch E, Herring PK. Challenges and opportunities for high-quality battery production at scale. Nat. Commun. 2025;16:611.

- Chen SR, Zhou MZ, Zhao X, et al. Space-efficient protection for cylindrical batteries embedded into multi-cell structures: Evaluation and mechanistic investigation. Thin-Walled Struct. 2024;197:111630.

- Rusch KC. Energy-absorbing characteristics of foamed polymers. J. Appl. Polym. Sci. 1970;14:1433-1447.

- Liu K, Liu YY, Lin DC, et al. Materials for lithium-ion battery safety. Sci. Adv. 2018;4:9820.

- Liu S, Wang S, Sang M, et al. Nacre-mimetic hierarchical architecture in polyborosiloxane composites for synergistically enhanced impact resistance and ultra-efficient electromagnetic interference shielding. ACS Nano 2022;16(11): 19067-19086.

- Liu YL, Li B, Xu MJ, et al. Highly efficient composite flame retardants for improving the flame retardancy, thermal stability, smoke suppression, and mechanical properties of EVA. Materials 2020;13(5):1251.

- Li XF, Zhang D, Xiang KW, et al. Synthesis of polyborosiloxane and its reversible physical crosslinks. Rsc Advances 2014;4(62):32894-32901.

- Yang HW, Tu H, Yang Z, et al. Micromechanical properties of shear stiffening gel reinforced ethylene–vinyl acetate foam. Materials Letters 2023;351:134993.

- American Society for Testing and Materials (ASTM). ASTM C518-21: Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus (S). West Conshohocken, PA: American Society for Testing and Materials (ASTM), 2021.

- Underwriters Laboratories (UL). UL 94-23: Standard Test Method for Flammability of Plastic Materials for Parts in Devices and Appliances (S). West Conshohocken, PA: Underwriters Laboratories (UL), 2023.

- Chordiya YM, Goel MD, Matsagar VA. Assessment of energy absorption for different foams subjected to low-velocity impact. Sādhanā 2023;48:157.

- Xing YQ, Guo XY, Shu GW, et al. Dynamic crushing behavior of ethylene vinyl acetate copolymer foam based on energy method. Ploymers 2023;15(14):3016.

- Xing YQ, Sun DQ, Zhang MY, et al. Crushing responses of expanded polypropylene foam. Polymers 2023;15(9):2059.

- Wang ZL, Liu Z, Liu YZ, et al. On the crush behavior and energy absorption of sustainable beverage cans and their polyurethane foam-filled structures: An experimental study. Materials 2024;17(11):2655.

- Deb A, Shivakumar ND. An experimental study on energy absorption behavior of polyurethane foams. J Reinf Plast Comp 2009;28(24): 3021-3026.

- Saha MC, Mahfuz H, Chakravarty UK, et al. Effect of density, microstructure, and strain rate on compression behavior of polymeric foams. Mater. Sci. Eng.A 2005;406:328-326.

- Fan JQ, Xin K, Cai CL, et al. Experimental study of quasi-static mechanical characteristic of polyurethane foam material. Journal of Experimental Mechanics 2011;26(2): 139-145.

- Wang H, Xie SC, Jing KK, et al. Closed-cell polyurethane in-situ foaming honeycomb for enhanced energy absorption and water intrusion resistance. Alex. Eng. J. 2025;114: 572-587.

- Ch SC, Rao RN. Energy absorption capabilities of cenosphere reinforced epoxy syntactic foams. Mater.Res.Express 2019;6:125303

- Ma Y, Peng ZL, Zhang YX. Compressive behavior and energy-absorption characteristics of natural rubber foams. China Synthetic Rubber Industry 2007;30:436-439.

- Koohbor B, Blourchian A, Uddin KZ, et al．Characterization of energy absorption and strain rate sensitivity of a novel elastomeric polyurea foam. Adv. Eng. Mater 2021;23:2000797.

- Cronin DS, Ouellet S. Low density polyethylene, expanded polystyrene and expanded polypropylene: Strain rate and size effects on mechanical properties. Polym. Test. 2016;53:40-50.

- Recht RF, Ipson TW. Ballistic perforation dynamics. J. Appl. Mech. 1963;​30:384-390.

- Gu HJ, Liu C, Liu Q, et al. High- and low-temperature resistant and intrinsically flame retardant poly(bisphthalazinone thioether sulfone ketone)s: Synthesis, structures and properties. Chem. Eng. J. 2023;​471:144480.

- Feng CM, Liang MY, Chen WJ, et al. Flame retardancy and thermal degradation of intumescent flame retardant EVA composite with efficient charring agent. Anal. Appl. Pyrolysis 2015;113:266-73.

- Yang CB, Sunderlin N, Wang W, et al. Compressible battery foams to prevent cascading thermal runaway in Li-ion pouch batteries. J. Power Sources. 2022; 541:231666.

- Kim, G.-H. & Pesaran, A.A. Battery Thermal Management System Design Modeling. Conference paper. Golden, CO: National Renewable Energy Laboratory (NREL); Series: NREL/CP; 2006;540-40446.